## Slide 1
X : Previous works.
X : Last / this week works.
X : Next week tasks.
Test Electrode Printing | 4 and 6 mil electrode printing | Print with Ag, Ag/AgCl, and Carbon inks | Optimization of printing process | Print Electrode on ES metal Oxide fiber | Experimental plane and procedure*
X | X | X | X | X | 
Sensing mechanism under illumination | Photocurrent measurement | CO sensing under red light | CO sensing under green light | CO sensing under UV light | CO sensing under low CO concentration | NO2 sensing under UV light | NH3 sensing under UV light | Data analysis | Find out right combination to reduce CO poisoning | Draft of paper and figures
X | X | X | X | X | X | X | X | X | X | X
Weekly sensor group meeting (05/16/2013)
Heng Chia Su
Task 1 : Reproduce SnO2/SWNTs CO sensor and study of Pt/SnO2/SWNTs hybrid structure
Task 4: Electropsinning metal oxide nanofiber for gas sensor under elevated temperature
Task2: Pt/SWNTs
CO Sensing from 25 ppm to 2000 ppm | Data Analysis | Regeneration at 170oC | CO sensing under higher applied Voltage | CO sensing under 9V applied Voltage | Test highest potential an apply for sensing | CO sensing at 3.5, 3, 2, and 1V | CO sensing at 3V under 100°C | Photocurrent measurement | NO2 , NH3 and H2 sensing under UV light | Data Analysis
X | X | X | X | X | X | X | X | X | X | X
Task3: Longevity of SnO2/SWNTs and regeneration
Align SWNTs | Deposition of SnO2 | Sensing as fabricate SnO2 | Method for regeneration |  |  | 
X | X | X | X |  |  | 

## Slide 2: Pt/SWNTs _ 1 mM Photocurrent Under UV Illumination In Air
-0.45V
-0.55V
-0.625V
0.00125 C/cm2
0.0125 C/cm2
0.125 C/cm2

## Slide 3: Pt/SWNTs toward CO Sensing _ 1 mM Under UV Illumination 5-200 PPM CO
-0.45V
-0.55V
-0.625V
0.00125 C/cm2
0.0125 C/cm2
0.125 C/cm2

## Slide 4: Pt/SWNTs toward CO Sensing_ 1 mM_ 5-200 ppm CO
-0.45V
-0.55V
-0.625V
0.00125 C/cm2
0.0125 C/cm2
0.125 C/cm2

## Slide 5: Pt/SWNTs toward CO Sensing _ 1 mM Under UV Illumination 0.05-5 PPM CO
-0.45V
-0.55V
-0.625V
0.00125 C/cm2
0.0125 C/cm2
0.125 C/cm2

## Slide 6: Pt/SWNTs toward CO Sensing _ 1 mM_NH3
-0.45V
-0.55V
-0.625V
0.00125 C/cm2
0.0125 C/cm2
0.125 C/cm2

## Slide 7: Pt/SWNTs toward CO Sensing _ 1 mM_NO2
-0.45V
-0.55V
-0.625V
0.00125 C/cm2
0.0125 C/cm2
0.125 C/cm2

## Slide 8: Pt/SWNTs toward CO Sensing _ 1 mM_H2
-0.45V
-0.55V
-0.625V
0.00125 C/cm2
0.0125 C/cm2
0.125 C/cm2

## Slide 9
 | Pt/SWNTs | SnO2/SWNTs | Pt/SnO2/SWNTs_ 1 mM | Pt/SnO2/SWNTs_ 10 mM
Effect of applied sensing voltage ( 1, 2, and 3V) | X | 1 and 2 V at 100 °C | 1 and 2 V at 100 °C | 1 and 2 V at 100 °C
Effect of temperature ( R.T. and 100 °C) | X | X | X | X
Effect of light illumination (Red, Green and UV) | UV | X | X | X
CO sensing